## Slide 1: Micro- en nanotechnology
Part 2 by Jessica de Wild (Jessica.deWild@uhasselt.be)

## Slide 2: Solar cells
Papers
Notes: I will start explaining what is ment with photoconversion efficiency and basic solar cells equations. Secondly, i will introduce the silicon solar cell world. The different techniques, and within that the interdigitated back contacts will be explained

## Slide 3: Solar energy
Solar Irradiance: power per unit area received from the sun
Total energy per m2 on earth: 1000 W/m2
Photon energy:

## Slide 4: Solar cells
Solar cells convert power from the sun (electromagnetic waves or ‘light’) into electrical power
Only light with photon energy higher than the band gap of the material is absorbed
https://en.wikipedia.org/wiki/Solar_cell

## Slide 5: Solar cells
Power output depends on the area:
Irradiance = 1000 W/m2  26% efficient solar cells delivers 260 W/m2
Nominal performance: Wp (Watt-peak)
https://en.wikipedia.org/wiki/Solar_cell
Solar panel of 1.6 m2 delivers 350 Wp
10 panels on the roof  3.5 kWp
Area of solar panels : 16 m2

## Slide 6: Solar market
https://www.ise.fraunhofer.de/content/dam/ise/de/documents/publications/studies/Photovoltaics-Report.pdf
Learning rate: every doubling in PV module production reduces the price by 25%

## Slide 7: Solar cells
PV production
https://www.ise.fraunhofer.de/content/dam/ise/de/documents/publications/studies/Photovoltaics-Report.pdf

## Slide 8: Photovoltaic materials
Different commercial technologies
-Si wafer technology (mono and multi-crystalline)
-thin film technology (a-Si, Cu(In,Ga)Se2, CdTe)
Emerging technology
-perovskite
Photon energy:
Various properties, applications, fabrication methods, costs etc

## Slide 9: Photovoltaic materials
Insulator
Semiconductor
Conductor
Conduction band
Conduction band
Conduction band
Valence band
Valence band
Valence band
Energy (eV)
is in the range of the photon energy coming from the sun

## Slide 10: Photovoltaic materials
Semiconductor
Conduction band
Valence band
Energy (eV)
After absorption of a photon a valence electron in the valence band is excited to the conduction band
Electrons in the conduction band are free electrons and conduct electricity
Electron leave a ‘hole’ behind in the valence band (a ‘hole’ is a place were there used to be an electron)
The amount of holes / electrons determined the doping of a semiconductor

## Slide 11: Doping
Intrinsic, p or n type doping
Conduction band
Valence band
When photon is absorbed, a hole (h) is left behind in the valence band and electron (e) is added in the conduction band  # of e = # of h
Doping can increase the concentration of 1 type of carrier
Dopant adding electrons  n-type semi-conductor, dopant adding holes  p-type semi-conductor

## Slide 12: Doping
Intrinsic, p or n type doping
Conduction band
Valence band
When photon is absorbed, a hole (h) is left behind in the valence band and electron (e) is added in the conduction band  # of e = # of h
Doping can increase the concentration of 1 type of carrier
Dopant adding electrons  n-type semi-conductor, dopant adding holes  p-type semi-conductor
3e- 4e- 5e-
p-type n-type
Doping increases the concentration several orders of magnitude
~1010  1013 - 1018

## Slide 13: Solar cells
Basic working principle:
  1) the generation of light-generated carriers;
  2) the collection of the light-generated carries to generate a current
  3) the generation of a large voltage across the solar cell
  4) the dissipation of power in the load and in parasitic resistances
https://www.pveducation.org/pvcdrom/solar-cell-operation/solar-cell-structure
Emitter: n-type (phosphor)
 high concentration electrons
Base: p-type (boron)
 high concentration holes

## Slide 14: Solar cells
Basic working principle:
  P region: high concentration of holes
  N region: high concentration of electrons
  Where n and p type regions are in contact:
    Creation on pn junction
    Electric field  carrier flow
p–n junction - Wikipedia
IV Curve | PVEducation

## Slide 15: Solar cells
Basic working principle:
  1) Creation of diode, current flows in one directions
p–n junction - Wikipedia
IV Curve | PVEducation

## Slide 16: Solar cells
Basic working principle:
  Light generated carriers increased the current flow and power is generated
  P = I*V
p–n junction - Wikipedia
IV Curve | PVEducation

## Slide 17: Solar cells
IV curve
https://www.pveducation.org/pvcdrom/solar-cell-operation/solar-cell-structure
The efficiency of a solar cell is determined as the fraction of incident power which is converted to electricity and is defined as:
Where: Voc is the open-circuit voltage; Isc is the short-circuit current; FF is the fill factor and η is the efficiency

## Slide 18: Photovoltaic materials
Schockley Queisser Limit
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424
Notes: Thermal equilibrium

## Slide 19: Si technology
Basic silicon solar cell

## Slide 20: Si technology
Processing

## Slide 21: Si technology

## Slide 22: Si technology
Basic silicon solar cell
Silicon wafer: light absorbing material
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
~ 150 -200 µm

## Slide 23: Si technology
Wafer cleaning after cutting
Removal of sawing damage using KOH
Formation of pyramids during cleaning
  Light scattering properties
Notes: Potasium silicate and hydrogen

## Slide 24: Si technology
Formation of pn junction
Phosphor diffusion (n-type dopant) on p-type Si wafer
Boron diffusion (p-type dopant) on n-type Si wafer
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b

## Slide 25: Si technology
Diffusion electron contact (phosphor diffusion)
deposition of PSG
high temperature anneal  P diffusion
removal of PSG
POCl3 diffusion for industrial Si solar cell emitter formation Front. Energy 2017, 11(1): 42–51
PSG = Phosphosilicate glass (PSG)
Notes: Oxidation to passivate the surface

## Slide 26: Si technology
Diffusion electron contact
POCl3 diffusion for industrial Si solar cell emitter formation Front. Energy 2017, 11(1): 42–51
High thermal budget!
Depth
n
p

## Slide 27: Si technology
Front surface passivation
Surfaces are areas where charges recombine due to dangling bonds  making these inactive or reducing = surface passivation
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b

## Slide 28: Si technology
Passivation and anti-reflection: SiNx (SiOx)
SiNx passivated the dangling bonds (is a di-electric)
https://www.iue.tuwien.ac.at/phd/entner/node14.html

## Slide 29: Si technology
Passivation and anti-reflection: SiNx
SiNx passivated the dangling bonds (is a di-electric)
Serves as anti-reflection layer when correct thickness is applied
https://www.pveducation.org/pvcdrom/design-of-silicon-cells/anti-reflection-coatings
Optimal thickness ~ 70 nm

## Slide 30: Si technology
Metal contacts to extract the carriers
Metals are not transparent
  At the front: optical and electrical optimization by width and height
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b

## Slide 31: Si technology
Back contact: metallic layer and p++ doping
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b

## Slide 32: Si technology
Metallization: screen printing
https://www.appliedmaterials.com/files/Screen_Printing_Backgrounder_0.pdf

## Slide 33: Si technology
Contact formation front and back metal: firing
Front contact: Ag paste (to contact with the n-type Si)
Back contact: Al paste (also p-type dopant)
Ag paste etches through the SiNx layer
The SiNx layer will crystalize  improving passivation properties
High thermal budget!
n
p
p++

## Slide 34: Si technology
Contact formation: firing
Back: Al diffuses into Si layer, making a back surface field (diffused hole contact)
3e- 4e- 5e-
p-type n-type

## Slide 35: Si technology
Contact formation: firing
Back: Al diffuses into Si layer, making a back surface field (diffused hole contact)

## Slide 36: Si technology
Towards high efficiency and low cost:
Reduce optical and electrical losses and reduce thermal budget
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
https://www.pveducation.org/pvcdrom/design-of-silicon-cells/optical-losses

## Slide 37: Si technology
Back contact passivation di-electric layer to reduce the defect at the Si/metal interface
Contact in the di-electric layer are required for carrier flow  laser ablation
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b

## Slide 38: Si technology
Rear contact:
Appl. Phys. Rev. 7, 041315 (2020); https://doi.org/10.1063/5.0005090
Passivation: low surface recombination velocity on p-type silicon surfaces.
Optics: high internal reflection.
Electrics: compatibility with screen printing and firing processes.

## Slide 39: Si technology
Appl. Phys. Rev. 7, 041315 (2020); https://doi.org/10.1063/5.0005090
Towards high efficiency and low cost:
Reduce optical and electrical losses and reduce thermal budget

## Slide 40: Solar cells
Interdigitated back contact: reduce optical losses due to metallic fingers at the front
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
Typical distance ~ 10s of micron
Notes: Hit solar cells: low temperature processing, good passivation

## Slide 41: Si technology
Appl. Phys. Rev. 7, 041315 (2020); https://doi.org/10.1063/5.0005090
Phosphorus diffusion (n-type front contact): ~ 800 ºC
Firing metal contacts (front and back): ~ 800 ºC
Towards high efficiency and low cost:
Reduce optical and electrical losses and reduce thermal budget

## Slide 42: Solar cells
HIT cells: reducing thermal budget
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
2nd labo (TCO’s)
n-type
Notes: Hit solar cells: low temperature processing, good passivation

## Slide 43: Solar cells
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
HIT cell: heterojunction with intrinsic thin layer
Crystalline silicon (c-Si)
Amorphous silicon (a-Si)
Amorphous silicon
Notes: Hit solar cells: low temperature processing, good passivation

## Slide 44: Solar cells
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b
HIT cell: heterojunction with intrinsic thin layer
Crystalline silicon (c-Si)
Amorphous silicon (a-Si)
Amorphous silicon
Low deposition temperature
~ 200 deg
Low deposition temperature
~ 200 deg
Notes: Hit solar cells: low temperature processing, good passivation

## Slide 45: Si technology
Paper: combining HIT cells structure with interdigitated back contact
NATURE ENERGY 2, 17032 (2017) | DOI: 10.1038/nenergy.2017.32

## Slide 46: Solar cells
Interdigitated back contact
https://www.pveducation.org/pvcdrom/manufacturing-si-cells/rear-contact-solar-cells

## Slide 47: Solar cells
Paper: combining heterojunction and interdigitated back contact
NATURE ENERGY 2, 17032 (2017) | DOI: 10.1038/nenergy.2017.32
26.3%

## Slide 48: Solar cells
Paper: combining heterojunction and interdigitated back contact
NATURE ENERGY 2, 17032 (2017) | DOI: 10.1038/nenergy.2017.32

## Slide 49: Photovoltaic materials
Schockley Queisser Limit: maximum conversion energy depending on the band gap of single junction solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424

## Slide 50: Photovoltaic materials
Schockley Queisser Limit: maximum conversion energy depending on the band gap of single junction solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424
Maximum 33% can be converted into electric power

## Slide 51: Solar cells
Increasing efficiency further:
Tandem solar cells: stacked solar cells with different band gaps
https://www.pveducation.org/pvcdrom/tandem-cells
https://www.pveducation.org/pvcdrom/tandem-cells

## Slide 52: Solar cells
Increasing efficiency further:
Tandem solar cells: stacked solar cells with different band gaps
https://www.pveducation.org/pvcdrom/tandem-cells

## Slide 53: Solar cells
Tandem solar cells: Si + high band gap thin film solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424

## Slide 54: Solar cells
Record tandem cell 32.5%
Published: 28 September 2023
Enhanced optoelectronic coupling for perovskite-silicon tandem solar cells

## Slide 55: Next lectures
Week 4: no lectures / no labo
Week 5: Thin film PV technology and light management
Week 5 & 6: Solar cell labo (Diepenbeek)
NATURE ENERGY 2, 17032 (2017) | DOI: 10.1038/nenergy.2017.32
Papers in Toledo:
High-efficiency crystalline silicon solar cells: status and perspectives DOI: 10.1039/c5ee03380b