## Slide 1: Micro- en nanotechnology
Thin film deposition techniques and lithography

## Slide 2: MiNaT part 2
6 lectures
  Weeks: 1, 3, 5, 7, 9, and 11
  Literature: scientific papers (except introductory lecture)
Labo 4: solar cells and transparent conductive contacts
  Schedule of group1 / group 2
    Introduction November 17th, 9.30 @diepenbeek
    Labo 5: November 23nd /28th, 14.00 / 9:00 @ Energyville
    Labo 6: December 6th/7th 9.00 /14030 @ Energyville
    Travel time accounted for: 30 minutes
    Carpool sheet in toledo
One review paper (deadline 1st of December 23.59)
Reviewing deadline: 22nd of December 23.59
More info in toledo paper tab / lecturer 23th November and 7th December

## Slide 3: Energyville 2
Thor Park ~ 20 minutes ride

## Slide 4: Thin film deposition techniques
Si PV: thin film layers for passivation, anti-reflection, contacts, ..
Thin film PV: all layers are thin film

## Slide 5: Thin film deposition techniques
Wide variety of deposition techniques available
  Wet chemical:
    Screen printing; Chemical bath deposition
  Atomic layer deposition (ALD)
  Chemical vapour deposition (CVD)
    PECVD
  Physical vapour deposition (PVD)
    Sputtering; evaporation
Choice of method depends on costs, feasibility, throughput, thickness, homogeneity, quality of the film, required electrical properties, ....

## Slide 6: Thin film deposition techniques
Screen printing
Screen printing
Rear passivated Si solar cell
Plasma Enhanced
Chemical Vapour
Deposition (PECVD)
~ 10s nm
Atomic Layer Deposition (ALD) / lithography ~ 1-10 nm

## Slide 7: Thin film deposition techniques
Screen printing
Screen printing
Sputtering ~ 100s nm
Sputtering ~ 100s nm
Hetero-junction Si solar cell
PECVD ~ 10s nm
PECVD 10s nm

## Slide 8: Thin film deposition techniques
Sputtering ~ 100s nm
Chemical bath deposition ~ 10s nm
Evaporation ~ 1-3 µm
Sputtering ~ 100s nm
Thin film CIGS solar cell
https://www.solar-facts-and-advice.com/CIGS-solar-cell.html

## Slide 9: Thin film deposition techniques
Tandem solar cell

## Slide 10: Thin film deposition techniques
Tandem solar cell

## Slide 11: Thin film deposition techniques
Examples in solar cells:
  Wet chemical:
    CdS layers in CIGS
    Perovskite active layer
  Atomic layer deposition:
    AlOX passivation layer in Si solar cells
  Chemical vapour deposition:
    a-Si in Si heterojunction solar cells
    SiN2 SiOx passivation layers in Si solar cells
  Physical vapour deposition:
    Sputtering – TCO layers in all solar cells

## Slide 12: Thin film deposition techniques
Wet chemical: wet process step followed by drying step
  Chemical bath deposition (CBD) of CdS layer
Substrate will be submerged in aqueous solution
Stirring and heating of solution
Precursors in the solution reacts on the surface of the substrate
Thin film will grow on the surface

## Slide 13: Thin film deposition techniques
Wet chemical: wet process step followed by drying step
  Chemical bath deposition (CBD) of CdS layer
  Self limiting growth
  Thickness ~ 10s of nm depending on concentration, temperature and time
  Temperature 50-80 degrees (often water is used as liquid)
Cd+
S2-
CdS
Dry step: nitrogen flow, air flow, may include heating
CdS by CBD also cleans the CIGS surface and is preferential over CdS evaporation or sputtering

## Slide 14: Thin film deposition techniques
Wet chemical: (slot-die) coating
  Perovskite layer
https://www.perovskite-info.com/researchers-advance-slot-die-coated-perovskite-solar-cells-and-ink-properties
Most efficient perovskite solar cells are prepared by coating and is preferential over evaporation or sputtering

## Slide 15: Thin film deposition techniques
Atomic layer deposition: ALD
  Atomic layer deposition
Atomic Layer Deposition (ALD) / lithography ~ 1-10 nm

## Slide 16: Thin film deposition techniques
Atomic layer deposition: ALD
  Atomic layer deposition

## Slide 17: Thin film deposition techniques
Atomic layer deposition: ALD
  ALD saturation curve

## Slide 18: Thin film deposition techniques
ALD of AlOx
  Conformal coating
  Atomic thickness precision
  Low temperature
  Slow process
  High purity precursors required
Atomic Layer Deposition - ScienceDirect

## Slide 19: Thin film deposition techniques
Atomic layer deposition of AlOx
  Conformal coating
  Atomic thickness precision
  Low temperature
  Slow process
  High purity precursors required
Atomic Layer Deposition - ScienceDirect

## Slide 20: Thin film deposition techniques
CVD: exposure of the surface to precursors that react on the same surface. Usually, by products are produced
  SiN, SiOx
Materials 2021, 14(19), 5658; https://doi.org/10.3390/ma14195658
Plasma Enhanced
Chemical Vapour
Deposition (PECVD)
~ 10s nm

## Slide 21: Thin film deposition techniques
CVD: exposure of the surface to precursors that react on a surface. Usually, by products are produced
  a-Si (p and n-type doped)
Materials 2021, 14(19), 5658; https://doi.org/10.3390/ma14195658
PECVD ~ 10s nm
PECVD 10s nm

## Slide 22: Thin film deposition techniques
CVD: exposure of the surface to precursors that react on a urface. Usually, by products are produced
  Vacuum chamber with carrier gas (often Argon)
  (diluted) precursors enter the chamber
  Heated substate where the chemicals can react, and film will grow
  By-products and carrier gasses are pumped away from the chamber
https://www.mks.com/n/thin-film-deposition-overview
Notes: Ionized molecules - electrons

## Slide 23: Thin film deposition techniques
CVD: exposure of the surface to precursors that react on a surface. Usually, by products are produced
  a-Si growth (intrinsic, p and n-type)
  Gasses in: SH4 (silane), H2 and diluted in Ar
    For n-type a-Si: PH3
    For p-type a-Si: B2H6
  Si dangling bonds react Silane molecules
  Gasses pumped away: N2 and Ar
  Temperature between 150 – 300 °C
  Film growth and quality depends on temperature,
  concentration pre-cursers, flow in and out
SCIENTIFIC REPORTS | 5 : 9052 | DOI: 10.1038/srep09052
Notes: Ionized molecules - electrons

## Slide 24: Thin film deposition techniques
Sputtering ~ 100s nm
Sputtering ~ 100s nm
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Sputtering

## Slide 25: Thin film deposition techniques
Sputtering ~ 100s nm
Sputtering ~ 100s nm
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Sputtering and evaporation
Evaporation ~ few µm

## Slide 26: Thin film deposition techniques
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Evaporation
Coatings 2018, 8, 402
Materials to be deposited will be heated until evaporation temperature
  Sources to heat: e-beam, laser beam, electricity, ...
Particles will be released
Microscopic particles will be deposited onto the substrate
Dependent on melting point of deposited materails

## Slide 27: Thin film deposition techniques
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Co-Evaporation
Coatings 2018, 8, 402
Materials to be deposited will be heated until evaporation temperature
  Sources to heat: e-beam, laser beam, electricity, ...
Multiple source are heated simultaneously
Ratios between evaporation rates of different elements required careful tuning
Cu(In,Ga)Se2  Cu:(In,Ga) 1:1, Se in overpressure

## Slide 28: Thin film deposition techniques
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Sputtering or evaporation
Coatings 2018, 8, 402
Sputtering:
  High power is applied between sputter-target and substrate holder
  Neutral particles are ejected from the sputter-target due bombardment of high energy particles
  Microscopic particles are released with high energy
  Via collisions between the substrate and target energy is released
  Microscopic particles will be deposited onto the substrate
Notes: A negative voltage of typically − 300 V or more is applied to the target. This negative voltage attracts positive ions to the target ejecting particles from the target after collision

## Slide 29: Thin film deposition techniques
PVD: deposited materials goes from a condensed phase to a vapor phase and then back to a thin film condensed phase on the surface
  Sputtering
Coatings 2018, 8, 402
Magnetron sputtering:
  Utilize strong electric and magnetic fields to confine charged plasma particles close to the surface of the sputter target
  Higher density of ejected particles from the target
Notes: Magentron sputtering:

## Slide 30: Thin film deposition techniques
Evaporation vs sputtering
Scientific REPORTs | 7:45463 | DOI: 10.1038/srep45463
Notes: Distance from release of the particles to substrate, adhesion due to bombarbment,

## Slide 31: Thin film deposition techniques
Sputtering
  Electric power source:
    Direct (DC) vs alternating radio frequency current (RF)
    RF is required to avoid built in charges as the target are not conductive
https://www.aemdeposition.com/sputtering-targets-news/dc-sputtering-vs-rf-sputtering.html
DC: Conducting target, metals
Fast sputtering rate
RF: Insulating materials, semi-conductors
Slow sputtering rate (~20% of DC)
More expensive and complex
Notes: DC: metals, neatrial particles RF: Charge build-up on insulating targets can be avoided with the use of RF sputtering where the sign of the anode-cathode bias is varied at a high rate (commonly 13.56 MHz).

## Slide 32: Thin film deposition techniques
Sputtering
  DC: metals
  RF: semiconductors: ITO, Al doped-ZnO, CIGS, CuO, ....
  RF: insulators: AlOx, ZnO, NiO, ...
  Thickness ~ 10s nm to few micrometers thick
  Temperature ~ Room temperature, heated (passive or active)
  Non-conformal:
Handbook of Deposition Technologies for Films and Coatings (Third Edition)
Science, Applications and Technology, 2010, Pages 364-391, Chapter 8 - Atomic Layer Deposition
Notes: DC: metals, neatrial particles RF: Charge build-up on insulating targets can be avoided with the use of RF sputtering where the sign of the anode-cathode bias is varied at a high rate (commonly 13.56 MHz).

## Slide 33: Thin film deposition techniques
2 papers:

## Slide 34: Thin film deposition techniques
Sputtering: ITO DC vs RF
ITO target (10 wt% SnO2)
Base pressure (O2, Ar)
O2, Ar
Volume 352, Issues 9–20, 15 June 2006, Pages 1466-1470
Notes: Redia frequency, direct current

## Slide 35: Thin film deposition techniques
Sputtering: ITO DC vs RF
  Optical properties of ITO DC sputtered or RF sputtered
Volume 352, Issues 9–20, 15 June 2006, Pages 1466-1470
DC sputtered ITO
60 nm/min; 300 nm
RF sputtered ITO
20 nm/min; 300 nm
Pw = DC/RF power to sputter target
CO2 – concentration O2 in vacuum chamber
Notes: Transmission: different oxygen flow, also different power. RF took about xx times longer

## Slide 36: Thin film deposition techniques
Volume 352, Issues 9–20, 15 June 2006, Pages 1466-1470
Sputtering: ITO DC vs RF
  Optical properties of ITO DC sputtered or RF sputtered
    Opto-electrical properties (Rs and T) for different deposited layers
    Low Rs high T is required for good transparent conductive layer
Notes: Mass flow controllers
Turbo molecular pump

## Slide 37: Thin film deposition techniques
https://www.vonardenne.biz/en/company/press-events/industrial-tcos-for-shj-solar-cells/
Conductivity = σ (S/m)
Resistivity = ρ = 1/ σ (Ωm)
Resistance= R = ρ·t/A (Ω/m)
Sheet resistivity = Rs = ρ/t (Ω/sq)
t
A
Rs - sheet resistance
Free carriers (most often electrons e-)
Mobility of the free carriers (µe)
Concentration of the free carriers (n)
Conductivity σ = e-nµe

## Slide 38: Thin film deposition techniques
Volume 352, Issues 9–20, 15 June 2006, Pages 1466-1470
 RF sputtering gives best properties of the TCO layer
Transmission 84.1% 88.1%
Sputtering: ITO DC vs RF
  Optical properties of ITO DC sputtered or RF sputtered
    Low Rs,high mobility, and low carrier concentration is required for good transparent conductive layer
Notes: Mass flow controllers
Turbo molecular pump

## Slide 39: Thin film deposition techniques
ALD vs sputtering: ZnO
Thin Solid Films 516 (2008) 1523–1528
ZnO target
Precursors:
DEZ: diethyl-Zn water
Notes: . In this study, we prepared ZnO films with ALD using diethyl Zn (DEZ) as a metal precursor and water as a reactant

## Slide 40: Thin film deposition techniques
Atomic layer deposition: ALD
  Atomic layer deposition
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn

## Slide 41: Thin film deposition techniques
ALD vs sputtering: ZnO
Thin Solid Films 516 (2008) 1523–1528
ALD is about 20 times slower
1 cycle ~ 17 seconds
Notes: . In this study, we prepared ZnO films with ALD using diethyl Zn (DEZ) as a metal precursor and water as a reactant

## Slide 42: Thin film deposition techniques
ALD vs sputtering: ZnO
Thin Solid Films 516 (2008) 1523–1528
Electrical parameters highly dependent on the deposition method
Notes: Komt door krstiallijne structuur en defects. ZnO via ALD is erg puur, geen defected, grain boundaries etc. met sputter heb je hoge energetische deeltjes die botsen. etc

## Slide 43: Thin film deposition techniques
Why ALD?
  Conform layers
  Extreme thin layers
Very thin SnO2 ALD layer ‘closed’ the electron transport layers
C60 - evaporation
IZO - sputtering

## Slide 44
Take away messages:
  Wide range on thin film deposition techniques available
  Examples are shown that are used in solar cell technology
  Often multiple options are possible, choice depends on:
    Quality of deposited layers
    Deposition time
    Deposition temperature
    Conformality
    Thickness
    Deposition chamber
    Throughput
    Substrate size
     examples for ZnO and ITO layers
Next lecture: functional structures in thin films