## Slide 1: MINAT Lecture 5: Micro- and nanostructures in solar cells
Jessica de Wild (Jessica.dewild@uhassselt.be)

## Slide 3: Why ultrathin solar cells?
Less materials use
  200 µm  ~ µm absorber layer thickness
  Reducing processing costs and time
Options for making them flexible or semi-transparent

## Slide 4: Why ultrathin solar cells?
But: often less efficient or more expensive than Si
https://www.nrel.gov/pv/interactive-cell-efficiency.html

## Slide 6: Challenges in ultrathin PV
Light absorption limited by absorber layer thickness
Recombination of charges is higher at the contacts

## Slide 7: Absorption
2 µm
How much light is absorbed, depends on the thickness of the layer
For CIGS:

## Slide 8: Absorption
500 nm
How much light is absorbed, depends on the thickness of the layer
For CIGS:

## Slide 9: Challenges in ultrathin PV
Light absorption limited by absorber layer thickness

## Slide 10: Absorption
Back reflector: gives unabsorbed light a second change to be absorbed (double pass absorption)
500 nm
Back reflector

## Slide 11: Light management
Light scattering: increasing path length
Meer licht wordt geabsorbeerd

## Slide 12: Light management
Light scattering and back reflection: further increasing path length

## Slide 13: Absorption
Percentage absorbed light in 2 µm thin Si absorber layer

## Slide 14: State-of-the-art of ultrathin Si solar cells
Current generation of ultrathin Si absorber layers

## Slide 15: State-of-the-art of ultrathin Si solar cells
Current generation of ultrathin Si absorber layers (ref 23)

## Slide 16: State-of-the-art of ultrathin Si solar cells
Current generation of ultrathin Si absorber layers (ref 21)

## Slide 17: Light trapping
EQE spectra of cells with (solid curve) and without (dashed line) light trapping for difference thicknesses absorber layer
F: light trapping factor
Double pass: F = 2
Lambertian scattering:
F = 4n2
(n = refractive index)

## Slide 18: State-of-the-art of ultrathin GaAs solar cells
Current generation of ultrathin GaAs absorber layers

## Slide 19: State-of-the-art of ultrathin GaAs solar cells
Current generation of ultrathin GaAs absorber layers

## Slide 20: State-of-the-art of ultrathin CIGS solar cells
Current generation of ultrathin CIGSe absorber layers

## Slide 21: State-of-the-art of ultrathin CIGS solar cells
Current generation of ultrathin CIGSe absorber layers

## Slide 22: Transfer techniques of thin films
Thin film transfer to reflective substrates
ref 23

## Slide 23: Fabrication of nanostructures I
Nanosphere lithography
  Sub micron structures for light scattering
Self assembled micro/nano spheres deposited on surface
Spheres are used as lithograph mask or embedded in the solar cells
Notes: However, their cost and long exposure time limit their use to proof-of-concept devices on small areas. In the framework of solar cell fabrication, specific techniques are required to structure matter at the nanoscale while being low-cost, scalable (patterned area >15 x 15 cm2 ) and versatile

## Slide 24: Fabrication of nanostructures I
Nanosphere lithography
  Sub micron structures for light scattering
Notes: However, their cost and long exposure time limit their use to proof-of-concept devices on small areas. In the framework of solar cell fabrication, specific techniques are required to structure matter at the nanoscale while being low-cost, scalable (patterned area >15 x 15 cm2 ) and versatile

## Slide 25: Fabrication of nanostructures II
Nanoimprint lithography
  Sub micron structures for light scattering
Replicating micro or nanoscale pattern by stamping in a soft resist materials
Stamp often made using an expensive master molt containing the structures

## Slide 26: Fabrication of nanostructures II
Nanoimprint lithography
  Sub micron structures for light scattering

## Slide 27: Selective contacts
Insulator
Semiconductor
Conductor
Conduction band
Conduction band
Conduction band
Valence band
Valence band
Valence band
Energy (eV)
Vacuum level

## Slide 28: Selective contacts
Conduction band
Valence band
When photon is absorbed, a hole (h) is left behind in the valence band and electron (e) is added in the conduction band  # of e = # of h

## Slide 29: Selective contacts
2.  # of e = # of h, e-h pairs will be separated due to internal electric field
Electron contact
Hole contact
Conduction band
Valence band

## Slide 30: Selective contacts
Electron contact
Hole contact
Conduction band
Valence band
3.  e and h need to be collected at the contacts
Good contacts

## Slide 31: Selective contacts
Electron contact
Hole contact
Conduction band
Valence band
3.  e and h need to be collected at the contacts
Bad contacts

## Slide 32: Selective contacts
Selective contacts: blocking or rejecting one of the carriers (hole or electron)

## Slide 33: Future architectures for thin film solar cells
Single junction solar cells

## Slide 34: Future architectures for thin film solar cells
Tandem solar cells

## Slide 35: Take-away messages
Ultrathin solar cells have many variable application
  Flexible, semi-transparent, light weight
Efficiency of terrestrial thin film PV is lacking behind compared to Si wafer technology
  Si: 26.7%, CIGSe: 23.35%, Perovskite: 25.7%
Efficiency improvements are implemented in two ways:
  Increase the absorption
    Back reflector, light scattering and anti-reflection coatings
  Passivate the electron and hole contacts
    Selective contacts
Tandem solar cells increase the efficiency even further
  Two thin technologies, but may also be combined with Si wafer technology