## Slide 1: MINAT: Thin film Solar Cells - Micro-structures and transparent contacts
Jessica de Wild (Jessica.dewild@uhassselt.be)

## Slide 3: Thin film solar cells
2nd generation solar cells
Thin films: cheaper materials, less materials, can be made flexible and/or semi-transparent, can be integrated in buildings/vehicles/...
Thickness of the active layer ~ µm
3 main commercially available technologies: a-Si:H, Cu(In,Ga)Se2 and CdTe
1 emerging technology: perovskite
https://www.buildup.eu/sites/default/files/illustrations/bipvao2.png

## Slide 4: Thin film solar cells
Si vs thin film
  Si PV is based on wafers of about 200 µm thick
  Thin films are deposited on carriers
    Glass, plastics, metal foils

## Slide 5: Thin film solar cells
Substrate / superstrate
  Glass, plastic, metal sheets
TCO: transparent conductive oxide = front contact (back-contact for bi-facial cells)
Metal: back contact
Deposition techniques: chemical or physical vapour deposition, wet processing
Absorber layer: CIGS or intrinsic a-Si:H = active layer where electron-hole pairs are generated
Separation of carriers happen at the hole and electron contacts

## Slide 6: Thin film solar cells
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
200 - 400 nm
n-type a-Si:H
Metal contact
substrate
Metal contact
p-type Cu(In,Ga)Se2 (absorber layer)
2-3 µm
n-type CdS
Transparent conductive layer
Transparent conductive layer
Hole contact
Electron contact
Electron contact
Hole contact

## Slide 7: Thin film solar cells
a-Si:H: One of the first commercially available thin film solar technology. They have an unavoidable problem related to the amourphous material: it is unstable over time (Steabler Wronski effect). Making the layer thinner, reduces this degradation. Thickness of a-Si:H layer: 200 - 400 nm. Too thin to absorb all the light  light management techniques using micro-structures
Cu(In,Ga)Se2: one of the most effecient thin film solar cell technology. For large scale application, the element Indium (In) causes concern due to the multiple usage in electronics generally (i.e. touch screens). Thickness of CIGS layer in commerical solar panels: 2-3 µm  ultrathin (~500 nm) CIGS in development  passivation and light management required

## Slide 8: Short introduction optics
Light and interaction with matter
Refractive index
  Complex number: N = n + ik
    Real n: refractive index
    Complex k: extinction coefficient
Light diffraction
  Snellius’ law
https://en.wikipedia.org/wiki/Diffuse_reflection
Air
n1 = 1
CIGS
n2 ~ 3

## Slide 9: Short introduction optics
Light and interaction with matter
Refractive index
  Complex number: N = n + ik
    Real n: refractive index
    Complex k: extinction coefficient
https://en.wikipedia.org/wiki/Diffuse_reflection

## Slide 10: Short introduction optics
Light and interaction with matter
Refractive index
  Complex number: N = n + ik
Reflection and transmission
  Perpendicular incindence
Air
n1 = 1
CIGS
n2 ~ 3

## Slide 11: Short introduction optics
Light and interaction with matter
Refractive index
  Complex number: N = n + ik
Absorption coëfficiënt
λ is the wavelength of the light
t is the thickness of the medium the light is traveling through
Air
n1 = 1
CIGS
n2 ~ 3
λ

## Slide 12: Short introduction optics
Light and interaction with matter
Diffuse and specular reflection
https://www.olympus-lifescience.com/en/microscope-resource/primer/java/reflection/specular/
Mirror
White wall

## Slide 13: Short introduction optics
Light and interaction with matter
Diffuse and specular reflection
https://www.olympus-lifescience.com/en/microscope-resource/primer/java/reflection/specular/
Specular reflection
Diffuse reflection

## Slide 14: Short introduction optics
Light and interaction with matter
Diffuse and specular reflection
  Scattering
https://en.wikipedia.org/wiki/Diffuse_reflection

## Slide 15: Optical losses
Not all incoming light will be absorbed:
  Reflected or absorbed in inactive layers at the front  TCO’s and anti-reflection coating
  Insufficient absorption in active layer  Light scattering and back reflection
https://doi.org/10.1038/s41560-020-00714-4

## Slide 16: Optical losses
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
200 - 400 nm
n-type a-Si:H
Metal contact
substrate
Metal contact
p-type Cu(In,Ga)Se2 (absorber layer)
2-3 µm
n-type CdS
Transparent conductive layer
Transparent conductive layer
Inactive layers (do not generate current)

## Slide 17: Anti-reflection coating
superstrate
Transparent conductive layer
Transparent conductive layer

## Slide 18: Anti-reflection coating
superstrate
Transparent conductive layer
Transparent conductive layer

## Slide 19: Anti-reflection coating
Matching refractive indices to decrease reflection at the front

## Slide 20: Transparent conductive layers
superstrate
Transparent conductive layer
Transparent conductive layer

## Slide 21: Transparent conductive layers
Most used:
ITO: In2O3/SnO2
AZO: ZnO/Al
TCO: Transparent Conductive Oxide
Conductive materials: metals
Transparent materials: plastics and glass
Having both is actually kind of special
Labo2: optical and electrical properties of ITO, ZnO and etched ZnO

## Slide 22: Sheet resistivity
https://www.vonardenne.biz/en/company/press-events/industrial-tcos-for-shj-solar-cells/
Conductivity
Free carriers (most often electrons e- in the conduction band)
Mobility of the free carriers (µe) (cm2/(Vs))
Concentration of the free carriers (n) (cm-3)
Conductivity σ = e-nµe

## Slide 23: Sheet resistivity
https://www.vonardenne.biz/en/company/press-events/industrial-tcos-for-shj-solar-cells/
Conductivity = σ (S/m)
Resistivity = ρ = 1/ σ (Ωm)
Resistance= R = ρ·t/A (Ω/m)
Sheet resistivity = Rs = ρ/t (Ω/sq)
t
A
Conductivity
Free carriers (most often electrons e-)
Mobility of the free carriers (µe)
Concentration of the free carriers (n)
Conductivity σ = e-nµe

## Slide 24: Sheer resistivity
Resistance in solar cell
  Voltage losses Vloss = IR
  Fill factor losses  squareness of the JV curve

## Slide 25: Sheet resistivity
https://www.vonardenne.biz/en/company/press-events/industrial-tcos-for-shj-solar-cells/

## Slide 26: Transparency
Free carriers tend to absorb light
 low concentration of carriers and high mobility
More Al, more free carriers, less transparent
 Losses of incoming light

## Slide 27: Optical losses
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
200 - 400 nm
n-type a-Si:H
Metal contact
substrate
Metal contact
p-type Cu(In,Ga)Se2 (absorber layer)
2-3 µm
n-type CdS
Transparent conductive layer
Transparent conductive layer
500 nm

## Slide 28: Absorption
2 µm
How much light is absorbed, depends on the thickness of the layer
For CIGS:

## Slide 29: Absorption
500 nm
How much light is absorbed, depends on the thickness of the layer
For CIGS:

## Slide 30: Light management
Light scattering and back reflection: lengthen optical path is absorber layer
Increased path length:
More light is absorbed

## Slide 31: Light management
Light scattering incoming light: lengthen optical path is absorber layer

## Slide 32: Light management
Back reflector: reflect light back into the absorber layer

## Slide 33: Quantum efficiency
How to determine the increased path length?
  Increase pathlength should lead to increased current generation
  Usually the absorbance of longer wavelength are increased
  External Quantum Efficiency (EQE) measurements are good tool to determine increased absorption
https://en.wikipedia.org/wiki/Quantum_efficiency

## Slide 34: Quantum efficiency
https://www.pveducation.org/pvcdrom/solar-cell-operation/quantum-efficiency

## Slide 35: Light scattering
TCO: random growth of crystals
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
500 nm
n-type a-Si:H
Metal contact
Transparent conductive oxide

## Slide 36: Light scattering
TCO: etching
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
500 nm
n-type a-Si:H
Metal contact
Transparent conductive oxide

## Slide 37: Back reflector
Increase the reflection at the back
  Matching refractive indices
  Low k materials: N = n + ik
    N2 low and k (absorption) low
    When k is high  absorption
  Metals: low n high k
    Absorption of light instead of reflection
Intrinsic a-Si:H
(absorber layer)
500 nm
n-type a-Si:H
Metal contact
N1
N2

## Slide 38: Back reflector
Increase the reflection at the back
  Matching refractive indices
  Low k materials: N = n + ik
    N2 low and k (absorption) low
    Insertion of low k and low n layer (ZnO)
Intrinsic a-Si:H
(absorber layer)
500 nm
n-type a-Si:H
Metal contact
N1
N2
N2

## Slide 39: Thin film Si cells
Increase optical light path by scattering
  Textured TCO layers
Impact of front and rear texture of thin-film microcrystalline silicon solar cells on their light trapping properties
Hitoshi Sai (齋均,a Haijun Jia (賈海軍, and Michio

## Slide 40: Back reflector / light scattering in CIGS
substrate
Metal contact
p-type Cu(In,Ga)Se2 (absorber layer)
500 nm
n-type CdS
Transparent conductive layer
Due to deposition method, light management techniqes are generally applied at the back contact (and may also suffice as passivation)

## Slide 41: Method
Lithography:
  Soft Nano-imprint
  Mask
https://www.researchgate.net/publication/41834415_Substrate_conformal_imprint_lithography_for_nanophotonics
https://onlinelibrary-wiley-com.bib-proxy.uhasselt.be/doi/epdf/10.1002/solr.201800212

## Slide 42: Light management in CIGS
Imprinting:
10.1021/acsnano.5b04091
SiO2 is a dielectric and also has passivating properties  contact with Mo required

## Slide 43: Metallic nanoparticles
Particle absorbs and re-emits light  spherical emitter
  Wavelength of highly scattered light depends on the particles size
Wavelength λ
Particle size with circumference 2πr

## Slide 44: Metallic nanoparticles
Particle absorbs and re-emits light  spherical emitter
  Wavelength of highly scattered light depends on the particles size
Wavelength λ
Particle size with circumference 2πr

## Slide 45: Metal nanoparticles
Small metal nanoparticles have high scattering properties

## Slide 46: Method
Gold nanoparticles encapsulated in AlOx
AlOX is also a dielectric with very good passivating properties

## Slide 47: Light management in CIGS
Al2O3  passivation and encapsulation
Gold nanoparticles  light scattering particles

## Slide 48: Light management in CIGS
Light scattering by thermally induced roughness
  During CIGS growth, the thin Ag and AlOx layers react with the CIGS layer and induce roughness at the back

## Slide 49: Light management in CIGS
Ag/AlOx: During CIGS growth, the thin Ag and AlOx layers break and induce roughness at the back
substrate
Metal contact
p-type Cu(In,Ga)Se2 (absorber layer)
500 nm

## Slide 50: Beyond single junction solar cells
Shockley Queisser Limit: maximum conversion energy depending on the band gap of single junction solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424

## Slide 51: Beyond single junction solar cells
Schockley Queisser Limit: maximum conversion energy depending on the band gap of single junction solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424
Maximum 33% can be converted into electric power

## Slide 52: Beyond single junction solar cells
Increasing efficiency further:
Tandem solar cells: stacked solar cells with different band gaps
https://www.pveducation.org/pvcdrom/tandem-cells
https://www.pveducation.org/pvcdrom/tandem-cells

## Slide 53: Beyond single junction solar cells
https://www.pveducation.org/pvcdrom/tandem-cells
Increasing efficiency further:
Tandem solar cells: stacked solar cells with different band gaps

## Slide 54: Tandem structures
Tandem solar cells: Si + high band gap thin film solar cell
Photovoltaic materials: Present efficiencies and future challenges DOI: 10.1126/science.aad4424

## Slide 55: Tandem structures
Perovskite / Si wafer
Pk band gap ~ 1.6 eV, deposition on top of Si wafer
Record tandem cell 32.5%
Published: 28 September 2023
Enhanced optoelectronic coupling for perovskite-silicon tandem solar cells

## Slide 56: Thin film solar cells
superstrate
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
200 - 400 nm
n-type a-Si:H
Metal contact
substrate
Metal contact
Transparent conductive layer
p-type a-Si:H
Intrinsic a-Si:H
(absorber layer)
200 - 400 nm
n-type a-Si:H
Transparent conductive layer
p-i-n
n-i-p

## Slide 57: Tandem structures
Thin film Si tandem structures
  a-Si:H band gap 1.7 eV, nc-Si band gap 1.1 eV

## Slide 58: Tandem structures
Thin film Si tandem structures
  a-Si:H band gap 1.7 eV, nc-Si band gap 1.1 eV
  Deposition order depending sub- or superstrate configuration
    Substrate: nip ns-Si, nip a-Si
    Superstrate: pin a-Si, pin nc-Si,
Glass
Glass

## Slide 59: Tandem structures
CIGS/perovskite
  CIGS and gap ~1 eV, Pk band gap ~ 1.6 eV
  Pk deposited on top of the CIGS layer after smoothening the ITO layer
Han et al., Science 361, 904–908 (2018) 31 August 2018

## Slide 60: Take away messages
Basic working principle of solar cells
Si technology and thin film technology -> advantages and disadvantages of the different technologies
Use of various materials and layers (active layer = absorber layer, non-active layers = contacts, emitters)
Optical losses and how to deal with it
Concept of tandem cells
Next lectures: deposition techniques, characterization techniques, passivation & light management structures

## Slide 61
Notes: Take away massages: 2 different technologies: thin film and Si, Si: thick robust, highly efficient, reached its limit: thin film –new, more options, less efficient but faster and cheaper to make. Can be combined with SI in tandem technologie, can be flexible, semi-transparent. What is an absorber layer, what is a TCO, why do we need light absorption etc